|  | Technical/ Material Specification | No. CD003-FT007-MS-01 Date: 01.11.2011 Rev. No. 0 Page 1 of 1 |
| --- | --- | --- |
| Product : Alloy Steel Hexagonal Bolts / Studs Material : SA-540 Gr. B22, Class1 Condition : Hot rolled / hot forged or cold finished Technical Requirement : The material furnished under SA-540 Gr. B22, Class1 shall meet the requirements of ASME B & PV Code II Part A specification A 962 / A 962 M-2001. Chemical Composition : As per Table below: A Element C Mn P S Si Cr Mo % Composition 0.39 - 0.46 0.65 - 1.10 < 0.025 ≤ 0.025 0.15 - 0.35 0.75 - 1.20 0.15 - 0.25 Product variation Over or Under, % B 0.02 0.04 0.005 0.005 0.02 0.05 0.02 The intentional addition of Bi, Se, Te, and Pb is not permitted. Unless otherwise specified, separate determinations may vary from the specified ranges, except that elements in any heat must not vary both above and below the specified range. Mechanical Properties : As per Table below; Tensile Strength MPa (min) Yield Strength MPa (min) Elongation % (min) Reduction in Area % (min.) Surface Brinell Hardness 1138 1034 10 35 321 - 401 Certified Mill Test Reports: Mechanical test report for each lot of Bolts / Studs Chemical analyses report of each lot of Bolts / Studs from a specific heat Tests: Bolts / Studs shall be visually examined as per ND-2582. Quality: Bolts / Studs shall have a workmanlike finish. Miscellaneous: Marking of Bolts / Studs shall conform to the article S9 of SA-540. Retest shall be conducted in accordance with the requirements specified in section 14 of SA-540. Certified Mill Test Reports, showing that Bolts / Studs have been made to the requirements as mentioned above and given in relevant sections of ASME and ASTM standard shall be submitted. Note: All certificates shall be in English. |