|  | Technical Specification | Ref. No. TS(1483-13)/X Rev.0 |
| --- | --- | --- |
|  |  | November 29, 2011 |
| ALLOY STEEL HEX. HEAD BOLTS, NUTS, STUDS & PLAIN WASHERS (A193-B7/A194-2H) The Alloy Steel Hex. Head Bolts & Studs shall be supplied in accordance with ASTM specification A-193-B7 & the Hex. Head Nuts shall be supplied in accordance with ASTM specification A-194-2H along with the following supplementary requirements. Material supplied shall conform to mandatory requirements of ASTM specification A 29. The quantity and sizes of the Fasteners will be as referred on page 2 of this technical specification A report on the chemical analysis of each heat shall be submitted A report on tensile test shall be submitted The Fasteners shall be supplied in quenched and tempered condition Grade and manufacturer’s identification symbols shall be applied to the head of the bolts as defined by the relevant section of the code. Manufacturer’s certificate, certifying that the Fasteners have been made to the requirements as mentioned above and as given in the relevant sections of the above mentioned ASTM specification shall be submitted. The Fasteners should be suitably packed in boxes and properly tagged. The box and tags shall carry the grade symbol for the material identification and the manufacturer identification mark or name. All certificates shall be in English and shall indicate the reference No. of this Technical Specification. |

|  | Technical Specification | Ref. No. TS(1483-13)/X Rev.0 |
| --- | --- | --- |
|  |  | November 29, 2011 |
| Material Specification, Quantity and Size (A193-B7/A194-2H) Fasteners shall be supplied in accordance with ASTM Specification A 193-B7/A194-2H and the supplementary requirements as referred on page 1 of this technical specification. Sr.# Description Size Qty. Alloy Steel Hex. Head Bolts (Fully Threaded) with 01 Hex. Nut & 01 Plain Washer. M14X30 mm 100 Sets -do- M16X75 mm 100 Sets -do- M16X100 mm 100 Sets -do- M20X85 mm 100 Sets -do- M20X130 mm 150 Sets Alloy Steel Studs (Fully Threaded) with 02 Hex. Nuts & 02 plain Washers M16X150 mm 100 Sets -do- M20X190 mm 200 Sets -do- M28X290 mm 350 Sets. -do- Dia.3/4" UNC, L=210 mm 100 Sets -do- Dia.7/8" UNC, L=275 mm 250 Sets -do- Dia.1" UNC, L=220 mm 100 Sets Alloy Steel Hex. Nuts M10, H=D 150 Pcs. -do- M12, H=D 100 Pcs. |