|  | Technical Specification | Ref. No. TS(1483-16)/X Rev.0 |
| --- | --- | --- |
|  |  | November 29, 2011 |
| STAINLESS STEEL HEX. HEAD BOLTS, NUTS & PLAIN WASHERS (A193-B8/A194-8) The Stainless Steel Hex. Head Bolts shall be supplied in accordance with ASTM specification A-193-B8 & the Hex. Head Nuts shall be supplied in accordance with ASTM specification A-194-8 along with the following supplementary requirements. A report on the chemical analysis of each heat shall be submitted. A report on tensile test shall be submitted. The Fasteners shall be supplied annealed and strain hardened conditions. The quantity and sizes of the Fasteners will be as referred on page 2 of this technical specification. Grade and manufacturer’s identification symbols shall be applied to the head of the bolts as defined by the relevant section of the code. Manufacturer’s certificate, certifying that the Fasteners have been made to the requirements as mentioned above and as given in the relevant sections of the above mentioned ASTM specification shall be submitted. The Fasteners should be suitably packed in boxes and properly tagged. The box and tags shall carry the grade symbol for the material identification and the manufacturer identification mark or name. All certificates shall be in English and shall indicate the reference No. of this Technical Specification. |

|  | Technical Specification | Ref. No. TS(1483-16)/X Rev.0 |
| --- | --- | --- |
|  |  | November 29, 2011 |
| Material Specification, Quantity and Size (A193-B8/A194-8) Stainless Steel Hex. Head Bolts & Nuts shall be supplied in accordance with ASTM specification A193-B8/A194-8 (latest edition) and the supplementary requirements as referred on page 1 of this technical specification. Sr.# Description Size Qty. Hex Head Bolts with 01 Hex. Nut & 01 Plain Washer M6X25 mm 400 Sets -do- M8X30 mm 600 Sets -do- M12X30 mm 600 Sets -do- M16X75 mm 500 Sets -do- Dia. 1-1/8” UNC, L=140mm 100 Sets Hex. Nuts M10, H=D 200 Pcs. -do- M12, H=D 200 Pcs. -do- M16, H=D 200 Pcs. |