|  | Technical Specification | Ref. No. TS(1483-15)/X Rev.0 |
| --- | --- | --- |
|  |  | November 29, 2011 |
| ALLOY STEEL SOCKET HEAD CAP SCREWS (A-574M) Alloy Steel Socket Head Cap screws shall be supplied in accordance with ASTM specification A-574M (latest edition) along with the following supplementary requirements. A report on the chemical analysis of each heat shall be submitted. A report on tensile test shall be submitted. The Screws shall be supplied in quenched and tempered condition. The quantity and sizes of the Screws will be as referred on page 2 of this technical specification. Grade and manufacturer’s identification symbols on all screws with nominal diameters of 5 mm and larger shall be applied to the side of the head or on top of the screws as defined by the relevant section of the code. Manufacturer’s certificate, certifying that the Screws have been made to the requirements as mentioned above and as given in the relevant sections of the above mentioned ASTM specification shall be submitted. The Screws should be suitably packed in boxes and properly tagged. The box and tags shall carry the grade symbol for the material identification and the manufacturer identification mark or name. All certificates shall be in English and shall indicate the reference No. of this Technical Specification. |

|  | Technical Specification | Ref. No. TS(1483-15)/X Rev.0 |
| --- | --- | --- |
|  |  | November 29, 2011 |
| Material Specification, Quantity and Size (A-574M) Alloy Steel Socket Head Cap screws shall be supplied in accordance with ASTM specification A-574M (latest edition) and the supplementary requirements as referred on page 1 of this technical specification. Sr.# Description Size Qty. Alloy Steel Socket Head Cap screws M2 X 0.4, L=20 mm 200 Pcs -do- M4 X 0.7, L= 25 mm 200 Pcs -do- M6 X 0.1, L=25 mm 200 Pcs -do- M8 X 1.25, L=25 mm 200 Pcs -do- M10 X 1.5, L= 45 mm 200 Pcs -do- M12 X 1.75, L= 60 mm 200 Pcs -do- M16 X 2.0, L=75 mm 200 Pcs |